## Slide 1
Automated design of hollowframe DNA origami nanostructures
A.J. Vetturini avetturi@andrew.cmu.edu
Professor Jonathan Cagan cagan@cmu.edu
Professor Rebecca E. Taylor bex@andrew.cmu.edu

## Slide 2: Nanostructure design automation broadens DNA origami accessibility
Introduction
Methodology
Results
Conclusions
Q&A
Level of Automation
Example CAD software
Typical Workflow
Scaffold
Staple
Optimize
Fully
vHelix6, DNAForge7, ATHENA suite8
Limited
caDNAno1, scadnano2
Semi
MagicDNA3, ENSnano4, inSequio5
Design barrier(s)
1. Douglas, S. M. et al. Nucleic Acids Research 37, no. 15 (2009): 5001–6.
2. Doty, D. et al. DNA 26, vol. 174 (2020).
3. Huang, C-M. et al. Nature Materials 20, no. 9 (2021): 9.
4. Levy, N. and Schabanel, N. DNA 27 (2021).
5. LaRock, C. et al. Preprint, bioRxiv (2024).
6. Benson, E. et al Nature 523, no. 7561 (2015): 7561
7. Elonen, A. et al. Nucleic Acids Research 52, no. W1 (2024): W13–18.
8. Jun, H. et al. Nucleic Acids Research 49, no. 18 (2021): 10265–74.
Notes: Broadens == ease of accesibility

## Slide 3: Specifically, materials research can benefit from automation
Introduction
Methodology
Results
Conclusions
Q&A
Goal
Periodic structure using DNA origami
Fully
Automated
Manual
TALOS1
Optimize
assembly
Design repeating unit
oxView: Poppleton, E. et al. Nucleic Acids Research 48, no. 12 (2020): e72.
caDNAno: Douglas, S. M. et al. Nucleic Acids Research 37, no. 15 (2009): 5001–6.
Mesh
Scaffold
Staple
Optimize
Iterate
1. Jun, H. et al. ACS Nano 13, no. 2 (2019): 2083–93.
Liu, H. et al. Science 384, no. 6697 (2024): 776–81.
Let’s design a material for …
Step 1
Step 2
Posnjak, G. et al. Science 384, no. 6697 (2024): 781–85.
Notes: Mention stiff enough particle

## Slide 4: However, not all geometries can be represented in current fully automated tools
Introduction
Methodology
Results
Conclusions
Q&A
Optimize
assembly
Design repeating unit
oxView: Poppleton, E. et al. Nucleic Acids Research 48, no. 12 (2020): e72.
caDNAno: Douglas, S. M. et al. Nucleic Acids Research 37, no. 15 (2009): 5001–6.
Fully
Automated
TALOS1
Mesh
Manual
Scaffold
Staple
Optimize
Iterate
1. Jun, H. et al. ACS Nano 13, no. 2 (2019): 2083–93.
Let’s design a material for …
Step 1
Step 2
Goal
Periodic structure using DNA origami
Response
Notes: Mention stiff enough particle

## Slide 5: HollowfrAme DNA Origami further expands this fully-automatable design space
Introduction
Methodology
Results
Conclusions
Q&A
1) Vertex-and-edge model
2) Specify N (i.e., thickness)
Input
Scaffold Routing
18
3
2
1) Initialize graph
N = 18
Notes: HADO gives access to thickness control and fully automated designs
HADO == Ryu

## Slide 6: HollowfrAme DNA Origami further expands this fully-automatable design space
Introduction
Methodology
Results
Conclusions
Q&A
2) Connect bundles
Goal
Rotate bundles minimizing total distance
1) Vertex-and-edge model
2) Specify N (i.e., thickness)
Input
Scaffold Routing
18
3
2
1) Initialize graph
3’ Ends
5’ Ends
2
2
1
N = 18
Notes: Each vertex form a linear assignment problem leveraging the directionality of DNA (The assignment problem consists of finding, in a weighted bipartite graph, a matching of maximum size, in which the sum of weights of the edges is minimum.)
The internal cycles are then connected using MST via a

## Slide 7: Mitering imparts global stiffness into the structure
Introduction
Methodology
Results
Conclusions
Q&A
Image from https://www.nationalassemblers.com/post/floor-trim-selection
Miter corners for flush fit
AA
AA
Top View
1
2
1
2
N = 18
35 nm
N = 18
35 nm
Without mitering, these designs would have similar outputs
For each connection, move towards shared vertex by 0.34 nm until thresold met
Notes: Emphasize / calrify scaffold routing (and not be knotted)

## Slide 8: Dynamic programming defines the staple set
Introduction
Methodology
Results
Conclusions
Q&A
Defaults set by 45K design analysis
1. Add staples and default crossovers
2. Select optimal break points to segment staples
a
min
s.t.
a > 5
b > 3
c > 3
b
c
Bundle
Ends
Bundle
Middle
Example grid of valid break points
(all in units of # nucleotides)
oxView: Poppleton, E. et al. Nucleic Acids Research 48, no. 12 (2020): e72.
caDNAno: Douglas, S. M. et al. Nucleic Acids Research 37, no. 15 (2009): 5001–6.

## Slide 9: HADO platform can be used across hollowframe / wireframe geometries
Introduction
Methodology
Results
Conclusions
Q&A
Example Designs
oxView: Poppleton, E. et al. Nucleic Acids Research 48, no. 12 (2020): e72.
1.0
4.0
RMSF (nm)
6HB Wireframe Comparison
HADO
TALOS-I
TALOS-M
Notes: Octet truss, BCC Truss, Hexa Prism, Anisotropic Y Junction

## Slide 10: Three sample designs illustrate the HADO paradigm
Introduction
Methodology
Results
Conclusions
Q&A
Input
Arrow
N=18
oxDNA Analysis
0.5
4.5
RMSF (nm)
Target: 75
Count
Y Junction
N=30
Target: 120
Count
oxView: Poppleton, E. et al. Nucleic Acids Research 48, no. 12 (2020): e72.
Tetrapod
N=18
Target: 109
Count
Angle Between Bundle (deg)
Notes: 30 HB: ~15 nm cavity
18 HB: ~10 nm cavity

## Slide 11: Three sample designs illustrate the HADO paradigm
Introduction
Methodology
Results
Conclusions
Q&A
0.0
5.0
nm
Tetrapod
Y Junction
Arrow
AFM scale consistent across all images | All scale bars 50 nm
N=18
N=18
N=30

## Slide 12: NUPACK used to define optimized sticky ends optimized for assembly
Introduction
Methodology
Results
Conclusions
Q&A
Generate valid combinations & screen melting temperature
Build NUPACK interaction matrix1
GPU-based simulated annealing to find optimal set of N seqs
1. Diep, T. et al. ChemRxiv 2025, no. 1224 (n.d.).
Filter:
M simulated
annealings in parallel
Notes: 250 choose 8 sequences is on order of 10^14
The matrix: NUPACK partion function for all pairs to get ensemble free energy (esf) value (kcal/mol) via NUPACK. A more negative (i.e., more blue) ensemble free energy means that the bound ensemble of strand a / b is favorable. A less negative (i.e., more yellow) means that they are less favorable. The diagonal in quadrant B is the strand + its reverse complement which is why that is most negative
Cross talk: Looking for largest energy difference between on target of sequence and the complements
Stacking: Looking for largest energy difference between sequences and themselves (ignoring complements)
Margin is adding the average binding energy of the set to the largest margin
ESF accounts for the contributions of all possible secondary structures and base-pairing probabilities,
Vecorization (JAX): Single Instruction, Multi-Data
Parallelization: Task-level concurrency (e.g., Multi-Instruction, Multi-Data)

## Slide 13: Overall, this work introduces a web-based, fully-automated platform for DNA origami
Automation driven via sequential optimization steps
Ability to parameterize bundle thickness
Design mesh inside inside streamlit GUI or import / use Python API
Introduction
Methodology
Results
Conclusions
Q&A
Response
Future: Embed symmetry + thickness into generative design1
1. Vetturini, A. J., Cagan, J. and Taylor, R. E. Nucleic Acids Research 53, no. 2 (2025): gkae1268.

## Slide 14
Questions?
Introduction
Methodology
Results
Conclusions
Q&A
Support
Vetturini, A. J., Cagan, J. and Taylor, R. E. In Preparation (2026).
Connect with me!
ajvetturini.github.io
Acknowledgements
Prof. James Conway (Pitt)
Anuhya Edupuganti (CMU)
Isabella Ferranti (CMU)
Vismaya Walawalker (CMU)
Read more about our groups
andrew.cmu.edu/user/bex/pages/welcome/
cmu.edu/me/idig/
Note: QR code likely inactive
Notes: National Defense Science and Engineering Graduate Fellowship

## Slide 15
Backup Slides

## Slide 16: DNA origami has been increasingly used in materials research
Introduction
Methodology
Results
Conclusions
Q&A
Wireframe
Mechanical Metamaterial4
Pyrochlore3
1. Posnjak, G. et al. Science 384, no. 6697 (2024): 781–85.
2. Wang, P. et al. JACS 138, no. 24 (2016): 7733–40.
3. Liu, H. et al. Science 384, no. 6697 (2024): 776–81.
4. Kulikowski, J. et al. Matter 7, no. 6 (2024): 2144–60.
Lattice-based
Diamond1
Plasmonic2

## Slide 17: The same annealing protocol was used for both 18HB and 30HB designs
Introduction
Methodology
Results
Conclusions
Q&A
Annealing Protocol
20 nM origami M13
200 nM staple mix
22 hr anneal
1X TAE @ 8.3 pH
N MgCl2
M13
(20 nM)
mM MgCl2
2
4
6
8
10
2
4
6
8
10
2
4
6
8
10
mM MgCl2
10
12
14
16
20
10
12
14
16
20
10
12
14
16
20
mM MgCl2
20
22
24
26
30
20
22
24
26
30
20
22
24
26
30
2% Agarose Gel run in 1X TAE for 75 min @ 100 V

## Slide 18: Measuring angles of oxDNA trajectory
Define which nucleotides belong to which bundle
Define which bundles should be measured
Fit a spline and measure the average angle between points for oxDNA trajectory
Trajectory
=

## Slide 19: Fitting staple default args using ~45k caDNAno designs
min
s.t.
a > 5
b > 3
c > 3
a
c
b
Target
a
b
c
Bundle
Ends
Bundle
Middle

## Slide 20: Fitting staple default args using ~45k caDNAno designs
min
s.t.
a > 5
b > 3
c > 5
a
c
b
Target
a
b
c
Bundle
Ends
Bundle
Middle

## Slide 21: Fitting staple default args using ~45k caDNAno designs
min
s.t.
a > 5
b > 5
c > 3
a
c
b
Target
a
b
c
Bundle
Ends
Bundle
Middle

## Slide 22: Fitting staple default args using ~45k caDNAno designs
c
Target

## Slide 23: Other assembly pictures